# www.beplas.com							                             Technical Data

# GPPA Adhesive

High Strength One part adhesive

# Product

GPPA is a high grab, one part MS Polymer based adhesive/sealant. GPPA is non-hazardous, does not contain Isocyanates, volatile organic solvents, acids or halogens. GPPA is odourless and Food Safe.

Good adhesion to glass, many kinds of metal (zinc, aluminium, steel), varnished and primed materials, wooden materials

Good resistance to humidity and weathering. Good adhesion to duroplastics, thermoplastics (except PE, PP, PTFE) and mineral substrates. Resistant to temperatures from -40(C to +80(C (up to +120(C for short intervals)

Purpose

GPPA is designed for high strength adhesive sealant applications and those exposed to aggressive environments and UV light. Solvent-free, elastic one component sealant and adhesive for bodywork, containers and vehicle manufacture, air conditioning, heating equipment, metalwork etc.

GPPA is ideal for use with Be-Plas Elite PVC and FRP panels.

Hand or battery operated applicators are available.

Design Data

| Code | Colour Options | Packaging | Viscosity |
| --- | --- | --- | --- |
| GPPA600 | White/clear | 600ml sachet 310ml cartridge | mastic |

Technical Data

| Base | Silane-terminated polymer, one component, curing with humidity |
| --- | --- |
| Colour | White, black, grey |
| Density | 1,60 g/cm³ | DIN 53 479 |
| Viscosity | Paste, spreadable with a blade or with a putty gun, good stability |  |
| Time for skin formation | 10min |  |
| Curing speed | 3mm (on the first day) Thicker layers require more curing time. | DIN 53 505 |
| Hardness Shore A | 55 specimen thickness 6mm, after 4 weeks | NK 23/50-2 |
| Elongation at break | 200 % | DIN 53 504 |
| Tensile strength | 2.3 N/mm² | DIN 53 504 |
| Tear resistance | 1.3 N/mm | ASTM D 624, Form B |

Processing temperature

+5°C to +30°C

Preparation

The surfaces to be bonded must be clean, dry and free of grease. Adhesion and compatibility must be individually tested when used on plastics or paint. GPPA 600 can be used without primer on most materials.

For strengthening the bond of absorbent materials such as wood and concrete, we recommend to use our primer.

Adhesion to non-absorbent surfaces can be increased by using primer for degreasing.

In that case, preliminary tests are required.

Bonding

Apply GPPA600 with a putty gun. The thickness of the layer depends on the types of material to be bonded and on the expected movement. Join the second material within 10 minutes and press. It is recommended to fix the bonded materials until the adhesive has cured. Curing speed depends on thickness of the adhesive layer, temperature and air humidity.

GPPA 600 is suitable for spraying with many varnishes immediately after application. After the skin formation of GPPA 600, adhesion problems may occur in case of some particular varnish systems.

Special Notes

Storage

Please do not store at temperatures of more than +25°C for longer periods of time. When stored in unopened containers, usable up to 12 months.

Safety

Please read our Safety Data Sheet and the labels of each product before use.

Pay particular attention to the directions given in Dangerous Substance Regulations.

Make sure the safety data sheet is readily available as it gives valuable information regarding the safe usage and disposal of the product and what to do in the event of an accident involving the product.

Freephone 0800 413 758 | Unit 2, Junction 8 Business Park, Ellesmere Port, Wirral, CH65 3AS